## Slide 1: Low Temperature Heat Capacity of the Frustrated Pyrochlore Magnets Gd2Hf2O7 and Gd2Zr2O7
Alice Durand
Professor L.R. Corruccini
Peter Klavins
University of California, Davis

## Slide 2: Introduction
Theoretically, pyrochlore lattices with isotropic anti-ferromagnetic exchange exhibit no magnetic order as temperature nears 0 K
We use the isotropic Heisenberg Hamiltonian to model the nearest neighbor interactions for such pyrochlores
(equation)
So far, the closest model systems have been Gd2Ti2O7 and Gd2Sn2O7 – both pyrochlores order magnetically at about 1/10 of the Curie-Weiss temperature. Even though these materials have identical crystal structures, they have different ground states.
These systems have been studied extensively by previous groups.

## Slide 3: Pyrochlore Lattice Diagram
Black dots = Gadolinium atoms

## Slide 4: Heat Capacity of Gd2Ti2O7
From P. Bonville et al.

## Slide 5: Heat Capacity of Gd2Sn2O7
P. Bonville et al., J. Phys.: Condens. Matter 15 (2003) 7777

## Slide 6: Introduction Continued
The long range order peaks in all of these materials implies that we need to take into account further-neighbor and dipole-dipole (potentially important for frustrated systems) interactions for the Hamiltonian.
Gd2Hf2O7 and Gd2Zr2O7 are a potentially useful third model system to study.
By measuring the heat capacity for Gd2Hf2O7 and Gd2Zr2O7, we discovered evidence of long-range ordering near 0.75 K in both the hafnium and zirconium pyrochlores.

## Slide 7: Magnetic Susceptibility for Gd2Hf2O7 and Gd2Zr2O7
Χ(t) yields a magnetic moment μ = 7.86μB, which is close to the free-ion value of μ = 7.94μB

## Slide 8: Lattice Constants
We can compare:
Gd2Hf2O7 : a = 10.515 Å
Gd2Zr2O7 : a = 10.522 Å
Curie-Weiss constant: θW ≈ -7 K (for both materials)
Gd2Ti2O7 : a = 10.184 Å
Gd2Sn2O7 : a = 10.460 Å
Curie-Weiss constant: θW ≈ -9 K (for both materials)
The Zr(+4) ion is ~1% bigger than the Hf(+4) ion, which accounts for the slightly larger lattice constant in the zirconate.

## Slide 9: Heat Capacity for Gd2Hf2O7

## Slide 10: Heat Capacity for Gd2Hf2O7
The sharp peak at TC ≈ 0.77 K is consistent with long-range magnetic order.
This peak is superimposed on the broad maximum centered at about 1 K, the latter indicating short-range order.
The peak maximum is about 17 J/mol-K, which is within 18% of the mean field prediction for a 2nd order magnetic phase transition for S = 7/2.
This magnitude of the heat capacity maximum for this material resembles Gd2Ti2O7 more closely than Gd2Sn2O7, where the transition is largely first-order with a peak amplitude that is roughly an order of magnitude higher, at ~100 J/mol-K.
θW /TC ~ 10 (similar to the stannate and titanate pyrochlores)

## Slide 11: Entropy for Gd2Hf2O7
The entropy of Gd2Hf2O7 approaches Rln(8)/mol at high temperatures.
Picture

## Slide 12: Heat Capacity for Gd2Zr2O7

## Slide 13: Heat Capacity for Gd2Zr2O7
The sharp peak is at TC ≈ 0.77 K, which is nearly identical to the hafnate and again consistent with long-range magnetic order.
Our results disagree with earlier measurements of the same material by S. Lutique et al., which showed no long-range order peak.
The difference is probably due to a longer annealing schedule for our samples.
The peak amplitude is larger than that of the hafnate, and is superimposed on a broad maximum whose amplitude is lower than in the hafnate.
The peak maximum is about 24 J/mol-K, which is again close to the mean field prediction for the 2nd order magnetic phase transition.
This heat capacity is qualitatively distinct from both the titanate and the stannate.

## Slide 14: Entropy for Gd2Zr2O7
The entropy of Gd2Zr2O7 approaches Rln(8)/mol at high temperatures.
Picture

## Slide 15: Comments
One surprising result for our heat capacity measurements is that the long-range order peak maximum for the Gd2Zr2O7 is much larger than that of the Gd2Hf2O7 , even though other investigators have associated greater crystalline disorder with the zirconate lattice
Rietveld refinements of both zirconium and hafnium pyrochlores give results consistent with some degree of cation disorder – at least 8% in Gd2Zr2O7
The differences between Gd2Zr2O7 and Gd2Hf2O7 are likely due to the 1% smaller radius of the Hf4+ ion – Gd3+ and Zr4+ are closer in size than Gd3+ and Hf4+.

## Slide 16: Conclusions
These materials resemble the titanate and the stannate in the degree of frustration present, but their heat capacities are distinct.
The nature of the ordered ground state for the hafnate and the zirconate remains to be determined