## Slide 1: Emissions from the Incineration of Electronics Industry Waste
E. S. Stewart, P. M. Lemieux
U.S. EPA
Research Triangle Park, NC

## Slide 2: The Electronics Waste Problem
According to OSW, at least 2.1 million tons of electronics waste (e-waste) was generated in 2000 (MSW in U.S. 2000 final report).
Of this amount, at least 1.9 million tons (91%) entered U.S. landfills or incinerators.
  E-waste may contain leachable toxic metals and brominated flame retardants.
  Some of the remaining waste ends up in recovery operations in developing nations.

## Slide 3
Scrap Wire Recycling in China

## Slide 4: Open burning of plastic encased metal printer and motor parts to reduce the waste to metals. Guiyu,China. December 2001. Copyright Basel Action Network.
Recovery of valuable metals
Source of PBTs
  PXDDs/Fs (?)
  Brominated Flame Retardants
E-waste Recycling in China

## Slide 5: Controlled E-waste Combustion
Tests conducted over a kiln temperature range of 570-830 °C
  Varied kiln preheat time
Heat generated from waste accounted for 17% of kiln firing rate.

## Slide 6: Flue Gas Measurements
Continuous emissions of O2, CO2, CO, NO
Volatile Organic Compounds (VOCs)
  On-line gas chromatograph
Sampling Trains
  Modified Method 5 (semi-volatiles)
  Method 26 (halogens)
  Method 23 (PCDD/Fs, PBDD/Fs)
  Method 29 (metals)

## Slide 7: Rotary Kiln Incinerator Simulator
TC
Main
Burner
Afterburner
Secondary Combustion Chamber(SCC)
CEMs
OLGC
M29
M26
CEMs
TC
TC
TC
TC
M23
TC
Primary Combustion
Chamber
Ram
Feeder

## Slide 8: The E-waste Feed
Waste was an equal parts (by weight) mixture of computer keyboards, motherboards, and cases.

## Slide 9: Feeding E-waste into Kiln

## Slide 10: Ultimate Analyses of Feed
 | Motherboards | Keyboards | Cases
C, % | 18.24 | 53.11 | 71.57
H, % | 1.63 | 5.14 | 7.01
N, % | 0.51 | 1.43 | 2.31
S, % | 0.09 | - | -
Br, % | 5.01 | - | 0.52
Cl, ppm | 1700 | 148 | 233
Ash, % | 66.79 | 28.68 | 8.63
KJ/kg | 6,958 | 31,005 | 28,028

## Slide 11: Kiln O2, CO2 Conc. – 11/20/02

## Slide 12: CO Concentrations – 11/20/02

## Slide 13: NO Concentration – 11/20/02

## Slide 14: VOC Conc. vs. Kiln Temperature

## Slide 15: Halogen Concentrations in Flue Gas

## Slide 16: Semi-volatile Organic Compounds
SVOC | Concentration, g/dscm
Naphthalene | 1.2-3.3
Acetophenone | 1.0-2.0
Chlorobenzene | 0.4-1.4
Dibenzofuran | 0.3-0.8

## Slide 17: Method 23 Results-PCDDs/Fs
No PCDDs were detected using LRMS
MCDF detected during low-temperature runs on 1/28 and 1/30/03 at 4ng/dscm.
OCDF detected during high-temperature run on 11/4/02 at 2 ng/dscm.

## Slide 18: Method 23 Results-PBDFs

## Slide 19: Polybrominated chloro-DFs

## Slide 20: Polybrominated dichloro-DFs

## Slide 21: PBDF Summary
Due to lack of standards, results for brominated and mixed bromochloro-DFs are semi-quantitative, at best.
Some brominated furans appear to be present in higher concentrations than those of MCDF.
  MBDF appears to be present at 5-10 X conc. of MCDF.
In general, PBDF > PB-MCDF > PB-DCDF

## Slide 22: Metal Concentrations in Flue Gas
Metal | Concentration, g/dscm
Copper (Cu) | 4600-7950
Lead (Pb) | 3790-4840
Antimony (Sb) | 790-1540
Cadmium (Cd) | 55-81
Manganese (Mn) | 19-52
Nickel (Ni) | 8-17
Barium (Ba) | 6-28
Arsenic (As) | 3-6
Chromium (Cr) | 3-4
Cobalt (Co) | 0.7-2.3
Beryllium (Be) | 0.1-0.3

## Slide 23: TCLP Results for Bottom Ash
 | 11/4/03 | 11/7/03 | EPA Max
As, ppm | 0.02 | 0.01 | 5.0
Ba, ppm | 0.534 | 0.790 | 100.0
Cd, ppm | 0.011 | 0.012 | 1.0
Cr, ppm | 0.138 | 0.043 | 5.0
Pb, ppm | 23.7 | 48.0 | 5.0
Hg, ppm | ND | ND | 0.2
Se, ppm | 0.013 | 0.015 | 1.0

## Slide 24: Summary
VOC emissions independent of kiln temperature over the range tested
  Primarily bromobenzene, other brominated organics
Emissions of PCDFs near detection limits of LRMS
PBDFs and mixed bromochloro-DFs were detected
Metal emissions were significant, consisting primarily of Cu, Pb, Sb, Cd, Mn

## Slide 25: Future Work: Open Burning of E-waste
Working with Baptist University in Hong Kong to determine size, type, and composition of e-waste
Scoping tests in open burn facility to quantify emissions of metals, VOCs, SVOCs, PXDDs/Fs